## Slide 1: 3D Probe Ptychography
Algorithm and preliminary results
Anders F. Pedersen
19-09-2018

## Slide 2: Setup
Sample: ρ
Focused beam (probe): Pj
Optical axis
Objective lens: Aperture: Ap Aberrations: Ab
z
y
x
Slit in image plane: S
Detector (far field)
2θ

## Slide 3: Parameters: Based on 3DBPP
Probe
  2D Gaussian (symmetric)
  Uniform phase (i.e. probe is real)
  Rastered in 2D, perpendicular to the beam direction
Sample
  Complex density
  Phase inspired from edge dislocation wall
  Fixed at central Bragg angle
  2θ=56°(Al(333))
  E=17keV
Objective lens
  CRL, N=70, fN=26.5cm
  Magnification, M=2
  Aperture and aberrations are separated
  Aperture is real 2D symmetric Gaussian
  Aberration is complex with magnitude 1 and variable phase
Slit
  Slit is placed in the image plane
  Slit function is 1 inside slit and 0 outside
  Slit is uniform along x
  Slit is scanned up and down along y

## Slide 4: Algorithm: Based on 3DBPP
Sample plane
Objective plane
Image plane
Detector plane

## Slide 5: Algorithm: Based on 3DBPP
Sample plane
Objective plane
Image plane
Detector plane

## Slide 6: Notes on the algorithm
: Fourier transform
: Projection operator, implemented in MatLab as mean(rho,3) along z
: Adjoint projection operator, implemented by repmat(rho,1,1,nz) along z in MatLab
The aperture is applied in both directions
  Stable algorithm, but resolution is probably limited to NA of lens
  Only updating the amplitude weighted by the aperture function with the measured amplitude is unstable
  So currently the amplitude is replaced by the measured amplitude (as is), as shown in the previous slide
Initial guess is typically zeros
  Some amplitude variations may occur where slit positions overlap. This can be suppressed in the algorithm, but it goes away on its own during the reconstruction.
The lens aberrations seems to be taken into account in the x-direction, but significant blurring is seen in the y-direction

## Slide 7: Reconstruction test
The object
  3.5 um wide
  Phase from edge dislocation wall, dislocations space 208 nm apart
  Dislocation wall tilts two halves by 0.079°
The beam
  Width of 195 nm (rms)
  Steps in 2D square grid of 263 nm step size (64% overlap)
The objective
  CRL, N=70, R=50 um, T=1.6 mm
  d1=42 cm, d2=93 cm, d3=3 m
  σa=209 urad (rms), M=2.08
The slit
  Opening 1.3 um (effective 625 nm)
  Step size 866 nm (effective 417 nm)
Datapoints
  Around 1800-1900

## Slide 8: Reconstruction test
Testing 4 different setups
  Lens aberrations, object phase
  Lens aberrations, no phase in object
  No aberration, object phase
  No aberration, no phase in object
This allows us to separate artifacts from the phase features, from the perfect reconstruction, and from lens aberrations

## Slide 9: Sample shape at 50% amplitude
True object
Lens aberrations Dislocation phase
No aberrations Dislocation phase
Lens aber. No phase
No aber. No phase

## Slide 10: True object (phase only for dislocation phase)

## Slide 11: Reconstruction: Lens aber. + disloc. phase

## Slide 12: Reconstruction: Lens aber. + no phase

## Slide 13: Reconstruction: No aber. + disloc. phase

## Slide 14: Reconstruction: No aber. + no phase

## Slide 15: Test: projection + probe without ptychography

## Slide 16: Strain in object
Positive strain
Negative strain

## Slide 17: Resolution analysis
X-direction
  30-40 nm (rms)
  Independent of aberrations
Y-direction
  20-30 nm (rms)
  Independent of aberrations
Z-direction
  175 nm (rms)
  Independent of aberrations
  Limited by beam size
Diagonal (semi-parallel to beam)
  100-105 nm (rms)
  Independent of aberrations
Diagonal (semi-perpendicular to beam)
  100-105 nm (rms)
  Independent of aberrations
Both diagonals limited by beam size

## Slide 18: Additional tests
All use objects with phase from dislocations and aberrated objective lens
Increased NA
  2x
  4x
  8x
Finite photon energy bandwidth
  (FWHM)
  Longitudinal coherence length:
  Optical path length difference:

## Slide 19: Additional tests: 3D renderings
NA – 2x
NA – 4x
NA – 8x
Partial coherence

## Slide 20: NA – 2x

## Slide 21: NA – 4x

## Slide 22: NA – 8x

## Slide 23: Partial coherence

## Slide 24: Resolution analysis
X-direction
  35 nm
  NA does not influence resolution
Y-direction
  NA 2x: 23 nm (rms)
  NA 4x and 8x: 9 nm (rms)
  Pixel size: 19.5 nm
  Partial coherence: 26 nm
Z-direction
  175 nm (rms)
  Still limited by beam size